## Slide 1
Stabilizing Ruthenium through Ru–O–Mn Interfacial Coupling for Acidic Oxygen Evolution
Final-year project · Progress review (first presentation)
Candidate
Zhao Shen
Programme
NUS–ECUST Joint Programme (MSE 311)
Supervisor
Prof. Xue Junmin, Materials Science and Engineering
Mentor
Yu Junchen, NUSRI-CQ
Date
24 September 2026

## Slide 2
Hydrogen: why the world is moving to it
About 100 Mt H2 a year; low-emission H2 is still under 1%.
The bottleneck is the route, not the molecule.
Data: IEA Global Hydrogen Review 2025 and 2026.
1

## Slide 3
Making hydrogen: two half-reactions
Cathode (HER): 2 H₂O + 2 e⁻ → H₂ + 2 OH⁻
Anode (OER): 2 H₂O → O₂ + 4 H⁺ + 4 e⁻
OER is the bottleneck
Four electrons and four protons: the slow half-reaction.
Two environments, two material sets
Alkaline: cheap Ni, Co or Fe. Acid (PEM): only Ir or Ru.
The anode limits the whole cell.
Panel: Chem. Soc. Rev. 2020, 49, 2196, Fig. 1 (re-rendered at high resolution).
2

## Slide 4
Three mechanisms side by side: what really differs
The three routes differ in two things: whether lattice oxygen is consumed, and whether one site or two adjacent sites perform the O–O coupling.
We target OPM: direct coupling needs no *OOH and leaves no vacancy, while LOM destroys the surface and AEM has an restriction.
Panels: Nat. Commun. 2023, 14, 354, Fig. 4d (AEM) and Supplementary Figs. 26 (LOM) and 35 (OPM), CC-BY.
3
Dual-site mechanism
Second site catalyzes
the second H2O
Lattice oxygen does not
participate
Lattice oxygen does not
participate
O catalyzes the
second H2O
OV catalyzes the
second H2O
Lattice oxygen
participates

## Slide 5
Mechanism I: AEM and its 0.37 V ceiling
The four steps
One site: H2O -> *OH -> *O -> *OOH -> O2.
Why it is capped
*OH and *OOH are locked together by a ~3.2 eV scaling gap.
Ideal steps are equal; real steps never are.
Floor ~ 0.37 V: AEM cannot go below it.
Chem. Soc. Rev. 2020, 49, 2196, Fig. 2a (adapted) · floor from Adv. Energy Mater. 2023, 13, 2301391, §3.2.
4

## Slide 6
Mechanism II: LOM pays with the surface
When it switches on
When O 2p rises to E_F, lattice O leaves as O2.
What is left behind
Vacancy left behind -> the metal dissolves in acid.
Mott-Hubbard: the O 2p band rises towards E_F.
LOM buys activity with the surface.
Adv. Energy Mater. 2023, 13, 2301391, Fig. 1e (Mott–Hubbard picture) and §4; vacancy-to-dissolution link as reviewed there, §6.
5

## Slide 7
Platform: why acidic PEM
PEM matches renewable electricity
High current density; the anode sees ~1 M H+ (pH 0).
Only Ir and Ru oxides survive there
In acid only Ir or Ru survive - and Ir is the scarcest.
This project is about durability at low noble-metal loading.
Panel: PEM electrolysis system review (cell schematic) · Chem. Soc. Rev. 2020, 49, 2196, §4.4.
6

## Slide 8
Element: Ru is active - but it dissolves
Why Ru and not Ir
More active than IrO2, far cheaper, more abundant.
Failure channel 1 — over-oxidation
Ru above +4 becomes soluble RuO4 and leaves.
Failure channel 2 — lattice oxygen
Lattice O leaves -> vacancy -> metal follows.
Both channels act together: stability is proved by dissolution numbers.
Adv. Energy Mater. 2023, 13, 2301391, Fig. 1g and §6 · Re-doped RuO₂: Nat. Commun. 2023, 14, 354.
7

## Slide 9
Solution: Ru inside a MnO2 framework
Mn³⁺/Mn⁴⁺ buffers the charge
Holds Ru near +4 - outside the RuO4 window.
The metal goes inside the lattice
It drives Ru in, forming M-O-Mn bridges.
Electrodeposition makes it tunable
Charge, current and bath pH set the phase.
Fig. 2: synthesis, structure and spectroscopy (a-h).
Our job: electrodeposit it and prove Ru sits inside.
Nat. Commun. 2026, 17, 7657, Fig. 2 · Science 2024, 384, 666, Fig. 1A (precedent with Ir).
8

## Slide 10
Experiment plan: deposit, window, exchange, prove, test
First priority: the host window (step 2).
Schematic drawn for this project: parameters per the group protocol; characterisation and testing practice follow Adv. Energy Mater. 2023 §5.
9